Experimental Notes for Reproducibility

To facilitate the accurate reproduction of the experimental procedures described in our article, "MOF-Derived Zr-Ce Solid Solutions with Engineered Oxygen Vacancies for Efficient Direct Synthesis of Dimethyl Carbonate from CO2," we provide the following practical insights based on our firsthand laboratory experience. These notes address critical variables that may affect experimental outcomes but are often overlooked in standard methodological descriptions.

1. Catalyst Preparation: Batch-to-Batch Consistency

The Ce-Zr composite oxide catalysts were synthesized via the calcination of Ce-Zr-MOF-808 precursors. We strongly recommend preparing and calcining multiple batches of precursors simultaneously rather than processing single batches sequentially. While minor batch-to-batch variations are inherent and widely accepted in materials synthesis, co-calcination effectively minimizes such discrepancies and ensures data reproducibility. According to our protocol, each batch yields approximately 1.1 g of precursor, which produces 0.5–0.6 g of catalyst after calcination—sufficient for only two catalytic runs. Therefore, parallel processing of multiple batches is essential to secure adequate material for systematic testing and validation.

2. Reaction Protocol: Heating Ramp and Activity Threshold

All reactions were conducted in a conventional high-pressure autoclave. It is important to note that the reaction times reported in the manuscript refer exclusively to the isothermal holding period and do not include the heating ramp, which typically requires 70–80 min in our setup. Although some reaction inevitably occurs during this ramping phase, control experiments in which the reactor was immediately cooled upon reaching the target temperature yielded negligible DMC production. This confirms that significant catalytic activity emerges only above ~125 °C under our conditions. Researchers attempting to reproduce these results should account for this thermal threshold when designing kinetic studies or comparing turnover frequencies.

3. Dehydrating Agent Quality: Critical Impact on Performance

The quality of the dehydrating agent (2-cyanopyridine) exerts a profound influence on catalytic performance, even among reagents labeled with identical nominal purity (≥99%). As illustrated in the figure below, the left vial contains a discolored (yellowish) batch, whereas the right vial shows a fresh, colorless batch (Adamas, LOT-P3513913-10454B). When tested over the same Zr0.05Ce0.95Ox-700 catalyst, these two batches produced markedly different results:

| catalysts | Conv. (%) | Yield (%) | Select(%) | Dehydrating Agent |
| --- | --- | --- | --- | --- |
| Zr0.05Ce0.95Ox-700 | 55.65197942 | 50.41399642 | 90.58796642 | left |
| Zr0.05Ce0.95Ox-700 | 65.5461279 | 64.04371015 | 97.70784668 | right |
| Zr0.05Ce0.95Ox-700 | 66.64541804 | 65.19153077 | 97.81847378 | right |

The discolored batch consistently delivered inferior conversion, yield, and selectivity. We therefore urge readers to inspect the physical appearance of 2-cyanopyridine prior to use and to document the supplier lot number in their experimental records. Discoloration likely indicates partial hydrolysis or oxidation during storage, which introduces impurities that competitively adsorb on active sites or alter the reaction medium. Sourcing fresh, colorless reagent from verified lots is essential for achieving the performance metrics reported herein.